## Slide 1
Low Temperature Aftertreatment (LTAT)
Test Protocol Development
  STEP 1
  Low-Temperature Oxidation
Reactor Description
Exhaust Simulation
Protocol Execution and Reporting
De-greening and Aging
ANALYTICAL
- [CO], [CO2], total HC, [NO], [NO2]
- [N2O], [NH3], stoich comb. [O2]
Frequency of Analysis
Sampling every 2°C
Rate of Response
≤ 15 seconds
TEMPERATURE MEASUREMENT
  REACTOR BASE-LINING
  Ensure reported data dictated solely by material behavior
  One-time blank run per application to base-line without catalyst
  Quantify recovery of reactive species to ensure fate
- catalyst inlet, within catalyst powder, inserted into core
Core Powder
PRE-TREATMENT
20 min @ 600°C
CDC, LTC-(D/G), L-GDI
– Lean [O2, H2O, CO2]
S-GDI
– Neutral [H2O, CO2]
ACTIVITY TESTING
2°C/min 100 – 500°C
30k GHSV (60k option)
Full simulated exhaust
  REPORTING
  Catalyst Sample Details
  Catalyst dimensions (or amount), composition
  Core substrate details (e.g., cell density)
  Reactor Configuration
  Reactor and heating details
  Details regarding thermocouple location, chemical analysis, sampling techniques, feed composition, GHSV
  Test Conditions
  Intended engine application
  Procedures used for de-greening, aging and/or poisoning, pre-treating & testing (or reference to protocol)
  Test Results/Performance Data
  Concentration versus temperature
  Conversion efficiency, T50/T90 determination
Gasoline
Diesel
CATALYST AGING – 800°C/50 hours
Time, seconds
  All catalysts de-greened prior to protocol execution
  De-greening once per sample; pre-treatment prior to each test
  Aging/poisoning to occur separately from activity testing
  Aged-state unchanged during the course of activity testing
DE-GREENING – 700°C/4 hours
Neutral – gasoline [S-GDI, L-GDI, LTC-G]
Lean – diesel [CDC, LTC-D]
PRE-TREATMENT
20 min @ 600°C
Sulfur Poisoning
POISON – 5 hrs @ 300°C
Full Simulated Exhaust
+ 5 ppm SO2
ACTIVITY
TESTING
Time, minutes
Diesel w/LNT – 800°C/10 hrs
The Advanced Combustion and Emission Control (ACEC) Technical Team
Low Temperature Aftertreatment (LTAT) working group
Including representatives from:
- FCA, Ford, GM, ORNL, PNNL, & DOE
The Protocol is a document that will be distributed via the CLEERS website upon final approval by USDRIVE leadership