## Slide 1
Hom Sharma
Ashish Mhadeshwar
Department of Chemical, Materials and Biomolecular Engineering
University of Connecticut , Storrs, CT
1 May 2012
A Detailed Microkinetic Model for Diesel Engine Emissions Oxidation on Pt DOC
1. http://enginecontrolsystems.com/images/homepage/ECSbroch_final.pdf
1

## Slide 2
Outline
Background : Diesel engine emissions
Emissions oxidation microkinetic modeling
  Mechanism development
  Kinetic parameter extraction
  Model performance
Model limitations
Future work
  Model expansion to larger emissions
  DOC deactivation due to sulfation

## Slide 3
CO (PPM) | HC (PPM) | NOX (PPM) | SOX (PPM) | DPM1 (g/cm3 )
5 – 1500 | 20 – 400 | 50 – 2500 | 10 – 150 | 0.1 – 0.25
3
Diesel emissions: Health and environmental impact
3.http://www.catf.us/diesel/problems/
2.http://en.wikipedia.org/wiki/File:Diesel-smoke.jpg
2
1.http://www.nett.ca/faq/diesel-1.html
4
4.http://www.fleetadvantage.net/effectsOfDiesel.cfm

## Slide 4
NOx: 0.2 g/bhp-hr
PM: 0.01 g/bhp-hr
NMHC: 0.14 g/bhp-hr
U.S. Clean Air Act Amendments of 1970:
a major shift in the federal government's role in air pollution control
Diesel engine emissions regulations
Heavy-duty highway engines
Emissions regulations are getting increasingly stringent.

## Slide 5
Diesel engine emissions aftertreatment system
Technologies to reduce Diesel engine emissions1
1.http://www.epa.gov/cleandiesel/documents/420r06009.pdf
NO:NO2 ratio
Oxidation of byproducts:
CO, HCN, CH2O, NH3

## Slide 6
Motivation for DOC modeling:
CO
NO
CH2O
NH3
HCN
Pt
DOC
Model
Pt/Pd based DOCs are expensive.
Fundamental understanding of DOC kinetics for emissions oxidation is necessary.
A detailed microkinetic model for DOC operation can be a good starting point for understanding DOC deactivation.

## Slide 7
Mechanism development
Parameter estimation
Model performance
Key steps in microkinetic modeling
CH2O*
H*
OH*
H2O*
CO*
CO2*
HCO*
CH2O(g)
A: Pre-exponential
Ea: Activation energy
Q: Binding energy
BI: Bond index

## Slide 8
Mechanism Development
Parameter Estimation
Model Performance
Steps in microkinetic modeling for emissions oxidation

## Slide 9
Mechanism development : 5 oxidation chemistries
HCN*
HCN(g)
CN *
O2(g)
O*
+O*
+O*
CO*
CO2*
H2O*
H2O(g)
OH*
N*
N2(g)
+O*
CO2(g)
NO*
NO2*
N2O*
NO2(g)
N2O(g)
Gas phase chemistry:
(GRI)1
Surface chemistry:
This work
21 Surface species
130 reactions
CHEMISTRY | REACTIONS
CO Oxidation | CO +1/2 O2  CO2
NO Oxidation | NO +1/2 O2  NO2
HCN Oxidation | HCN + O2  CO, CO2, NOx, H2O
NH3 Oxidation | NH3 +O2 NOx, H2O, N2
CH2O Oxidation | CH2O +O2  CO2, H2O
http://www.me.berkeley.edu/gri-mech

## Slide 10
Mechanism Development
Parameter Estimation
Model Performance
Steps in microkinetic modeling for emissions oxidation

## Slide 11
A
TST1
Desorption: 1013 s-1
Surface reaction: 1011 s-1
Literature
Sticking coefficients
Pre-exponential factors

TPD
DFT
Adsorbate interactions
Binding energies
Q
UBI-QEP2
DFT
TPD
E
UBI-QEP
TPR
Activation energies
Bond indices
BI
UBI-QEP
0.5
1. Dumesic, J. et al., The Microkinetics of Heterogeneous Catalysis,1998
Parameter estimation for the microkinetic model
2. Shustorovich, E. and Sellers, H., Surface Science Reports, 1998

## Slide 12
Parameter extraction from surface science experiments
Experimental data from literature
TPD/TPR on Pt
1D reactor model
Kinetic Parameters
Binding energies (Q)
Adsorbate interactions (α)
Bond indices (BI)
Activation Energies (Ea)
TPD
TPR
H2, O2, CO, CO2, N2, NO, NO2, H2O, CH2O, NH3, and HCN
CO, NO, CH2O, HCN, and NH3

## Slide 13: Parameter extraction from TPD experiments
QNO = 29.5 – 9.7NO kcal/mol
θinNO = 0.55 ML
0.05 ML
β = 10 K/s
Extracted parameters:
Binding Energy
Adsorbate interactions
NO TPD on Pt(111)
Literature range for QNO: 18-43 kcal/mol

## Slide 14
W. Ho and W. Mieher, Solid State Physics, 1995
θinNH3 = 0.12 ML
θinO = 0.25 ML
β = 2 K/s
Extracted parameters:
Bond indices
Activation energies
NH3 TPR
NH3*+O*  NH2*+OH*
NH2*+O* NH*+OH*
NH3*+OH*  NH2*+H2O*
NH*+O* N*+OH*
NH*+O*  NO*+H*
2NO*  N2O*+O*
2O* O2+2*
Parameter extraction from TPR experiments

## Slide 15
CH2O TPR
G.A. Attard, H.D. Ebert, and R. Parsons, Surface Science, 1990,
θinCH2O = 0.5 ML
θinO = 0.3 ML
β = 10 K/s
CH2O*+ *  HCO*+ H*
HCO*+O* CO*+OH*
HCO*+OH* H2O*+CO*
H2O*  H2O+*
CO*+OH*  CO2*+H*
OH*+H*  H2O*+*
2H*  H2+2*
CO*  CO+*
Mechanism validation against TPR experiments
Notes: Blank slide for drafting a body slide.

## Slide 16
Chart: Temperature [K]
0.5-Exp | 0 | 0 | 0.0015805 | 0.0073759 | 0.015805 | 0.026869 | 0.03846 | 0.052158 | 0.11169 | 0.15963 | 0.18598 | 0.18756 | 0.12117 | 0.040567 | 0.016859 | 0.0057953 | 0.0015805 | 0 | 0 | 0 | 0 | 0 | 0 | 0
0.25-Exp | 0 | 0.010094 | 0.033647 | 0.070658 | 0.087482 | 0.090847 | 0.094211 | 0.084117 | 0.053835 | 0.030282 | 0.0067294 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: Coverage Profiles
Chart: Temperature [k]
0.8-Exp | 0 | 0.012764 | 0.017869 | 0.026804 | 0.039567 | 0.051055 | 0.066371 | 0.0702 | 0.0702 | 0.068924 | 0.067647 | 0.062542 | 0.05616 | 0.049778 | 0.043396 | 0.031909 | 0.024251 | 0.015316 | 0.0089345 | 0.0063818 | 0.0012764 | 0 | 0 | 0 | 0 | 0 | 0
0.05-Exp | 0.00070577 | 0.0014115 | 0.0028231 | 0.0042346 | 0.0056462 | 0.0070577 | 0.00734 | 0.0070577 | 0.0063519 | 0.0056462 | 0.0042346 | 0.0028231 | 0.0014115 | 0.00070577
Chart: Temperature [K]
H2 TPD
N2 TPD
CO TPR
NO TPR
Chart: Temperature [K]
0.82-Exp | 0 | 0.0021035 | 0.011779 | 0.023138 | 0.039966 | 0.066469 | 0.091711 | 0.098862 | 0.10349 | 0.10475 | 0.10391 | 0.10055 | 0.094655 | 0.082455 | 0.076145 | 0.068993 | 0.055952 | 0.033235 | 0.026083 | 0.021035 | 0.013462 | 0.0050483 | 0
0.05-Exp | 0.00035685 | 0.0035685 | 0.0060665 | 0.0092781 | 0.01356 | 0.016415 | 0.017486 | 0.017486 | 0.016415 | 0.011776 | 0.0092781 | 0.0089213 | 0.0067802 | 0.0060665 | 0.0042822 | 0.0028548 | 0.002498 | 0.0007137 | 0.0010706 | 0.0007137
CO TPD
Additional examples

## Slide 17
Mechanism Development
Parameter Estimation
Model Performance
Steps in microkinetic modeling for emissions oxidation

## Slide 18
Mechanism/model performance:
Kinetic parameters are extracted from UHV TPD/R conditions.
DOC operating conditions are significantly different:
  Atmospheric pressure
  High flow rates
  Low emissions concentrations (ppm)
  Monoliths
  Fixed beds (literature experiments)
Mechanism/model performance should be tested under practically relevant conditions.
Isothermal plug flow reactor modeling at steady state.

## Slide 19
Model details
Fixed beds and Monoliths (PFR)
Oxidation of CO, NO, CH2O, HCN, NH3
Governing Equations for PFR:
Mass balance for gas species:
Surface species rate:
Site balance:
∑θk = 1
Sk = 0
Steady state
Isothermal
outlet
Inlet
Fixed Bed
Monolith
outlet
Inlet

## Slide 20
Model performance: CO oxidation on Pt
Experiments: K. Arnby, Journal of Catalysis, 2004.
Monolith:
1% CO
10% O2
SV = 17000 h-1
A/V = 32.6 cm-1
Pt/ZnO monolith:
1% CO, 10% O2,
89% Ar
Total flow = 50 sccm
SV = 30000 h-1
A/V = 30 cm-1
CO*
CO2*
O*
Literature experiments
Our experiments

## Slide 21
Experiments: D. Bhatia, R.W. McCabe, M.P. Harold, and V. Balakotaiah, Journal of Catalysis, 2009
NO*
NO2*
O*
Model performance: NO oxidation on Pt
Before thermodynamic consistency
After thermodynamic consistency

## Slide 22
Experiments: Crocoll, M, S Kureti, and W Weisweiler. Journal of Catalysis 229.2 (2005): 480-489.
Model validation: NO oxidation on Pt

## Slide 23
a. Experiments: C. Zhang, H. He, and K. Tanaka, Catalysis Communications, 2005
b. Experiments: J. Peng and S. Wang, Applied Catalysis B: Environmental, 2007
Model performance: CH2O oxidation on Pt

## Slide 24
CH2O oxidation on Pt: Reaction path analysis
CH2O*
CH2O(g)
HCO*
CO*
O2(g)
O*
+O*
+O*
+O*
CO2*
CO2(g)
OH*
+CO*
-H*
H2O*
H2O(g)

## Slide 25
Experiments: H. Zhao, R. Tonkyn, S. Barlow, B. Koel, and C. Peden, Applied Catalysis B: Environmental,. 2006
Model performance: HCN oxidation on Pt

## Slide 26
HCN*
HCN(g)
CN *
O2(g)
O*
+O*
+O*
CO*
CO2*
H2O*
H2O(g)
OH*
N*
N2(g)
+O*
CO2(g)
NO*
NO2*
N2O*
NO2(g)
N2O(g)
HCN oxidation on Pt: Reaction path analysis

## Slide 27
1. Experiments: Hakan Parsson, Selective catalytic oxidation of ammonia, 2004
http://www.chemeng.lth.se/exjobb/044.pdf,
Model performance and validation: NH3 oxidation on Pt

## Slide 28
NH3*
NH3(g)
NH2 *
NH*
O2(g)
O*
+O*
+O*
+O*
NO*
NO2*
H2O*
H2O(g)
OH*
N*
N2(g)
+O*
NO2(g)
-H*
N2O*
N2O(g)
NH3 oxidation on Pt: Reaction path analysis

## Slide 29
Summary
Emissions regulations are getting more stringent.
DOC modeling is challenging due to multiple emissions.
A microkinetic model is developed for oxidation of CO, NO, NH3, HCN, and CH2O on Pt.
Kinetic parameters are extracted from surface science experiments.
Model predicts various experimental data on monoliths and fixed beds, and can be used in DOC design.

## Slide 30
Microkinetic Model on Pt: Limitations and Future Work
CO
NO
NH3
CH2O
HCN
CO
NO
NH3
CH2O
HCN
CH3CHO
CH3CN
C2H4
Real engine exhaust compositions:
Mixture of CO,CO2,H2O,NO,NO2,NH3
DOC deactivation: Sulfur chemistry
Model expansion

## Slide 31
DOC deactivation due to sulfur
Support sulfation
Metal oxide sulfation

## Slide 32
DOE GAANN fellowship and Pre-doctoral fellowship
Prof. Pu-Xian Gao for Pt/ZnO monolith
Group members: Molly Koehle Venkatesh Botu Ameya Akkalkotkar
Acknowledgments